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PRODUCT SPECIFICATION



PRODUCT:				160mm x 22½° ESB Red Ducting Bend


ESB APPROVAL:			As per Spec 16113


MATERIAL - COLOUR:			PVC – Red


BEND RADIUS:				1,200mm 



AVE. OUTSIDE DIA (mm):		160.0 – 160.25



WALL THICKNESS (mm):		4.3 – 4.8



SOCKET:		Push Fit Socket on one end with Chamfer on 
		opposite end



ESB Code:				9317517			
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