DECLARATION OF PERFORMANCE

| Declaration number |  | MN 10 1/3/22 |  |  |
| --- | --- | --- | --- | --- |
| Unique identification code of the Product Type |  | 10 CON 0/10B MN |  |  |
| Registered name & address of the manufacturer |  | N&C Enterprises Ltd. Kilmeague Naas Co. Kildare, Ireland |  |  |
| Intended use |  | Aggregates for concrete |  |  |
| Relevant harmonised standard |  | I.S. EN 12620:2002+A1:2008 |  |  |
| System of assessment & verification of constancy of performance (AVCP) |  | 2+ |  |  |
| Name & identification number of the Notified Body |  | NSAI 0050-0940 |  |  |
| Declared performance |  |  |  |  |
| Properties relevant to the essential characteristics | Declared value/category |  | Properties relevant to the essential characteristics | Declared value/category |
| Size | 0/10 |  | Acid-soluble sulfate content | AS0.2 (SO4) |
| Grading | GA80 |  | Total sulfur content | S1 (actual < 0.1%) |
| Fines content | f3 |  | Water-soluble sulfate content | NPD |
| Shape of coarse aggregate | FI35 |  | Water-soluble chloride ion content | < 0.01% |
| Shell content of coarse aggregate | NPD |  | Acid-soluble chloride ion content of recycled aggregate | NPD |
| Resistance to fragmentation of coarse aggregate | LA30 |  | Carbonate content of fine aggregate | NPD |
| Resistance to wear of coarse aggregate | NPD |  | Constituents which alter the rate of setting/hardening of concrete | NPD |
| Particle density (app,od,ssd) | 2.64,2.56,2.59 Mg/m3 (approx.) |  | Constituents which affect the volume stability of slag | NPD |
| Water absorption | WA242 |  | Dangerous substances | NPD |
| Resistance to polishing of coarse aggregate | NPD |  | Resistance to freezing & thawing | MS25 |
| Resistance to surface abrasion of coarse aggregate | NPD |  | Drying shrinkage | < 0.075 % |
| Resistance to abrasion from studded tyres | NPD |  | Alkali-silica reactivity | Non-reactive |
| Classification of constituents of coarse recycled aggregate | NPD |  |  |  |

The performance of the product identified above is in conformity with the set of declared performance/s. This declaration of performance is issued, in accordance with Regulation (EU) No 305/2011, under the sole responsibility of the manufacturer identified above.

Signed for and on behalf of the manufacturer by Clement Gavin:    					     At Kilmeague, Naas, Co. Kildare, Ireland

(Signature)

This DoP covers only the harmonised/mandated properties listed in Table ZA.1 of  I.S. EN 12620.                                                                               Information regarding other properties is available on request.