DECLARATION OF PERFORMANCE

| Declaration number |  | MN 7/2 1/3/22 |  |  |
| --- | --- | --- | --- | --- |
| Unique identification code of the Product Type |  | 7 CON 0/4 MN |  |  |
| Registered name & address of the manufacturer |  | N&C Enterprises Ltd. Kilmeague Naas Co. Kildare, Ireland |  |  |
| Intended use |  | Aggregates for mortar |  |  |
| Relevant harmonised standard |  | I.S. EN 13139:2002 |  |  |
| System of assessment & verification of constancy of performance (AVCP) |  | 2+ |  |  |
| Name & identification number of the Notified Body |  | NSAI 0050-0942 |  |  |
| Declared performance |  |  |  |  |
| Properties relevant to the essential characteristics | Declared value/category |  | Properties relevant to the essential characteristics | Declared value/category |
| Size | 0/4 |  | Acid-soluble sulfate content | AS0.2 (SO4) |
| Grading | 0/4, MP |  | Total sulfur content | S1 (actual < 0.1%) |
| Fines content | Category 1 (≤ 3%) |  | Water-soluble chloride ion content | < 0.01% |
| Fines quality | NPD |  | Constituents which alter the rate of setting/hardening of mortar | XX |
| Shell content of coarse aggregate | NPD |  | Water-soluble matter of manufactured aggregate | NPD |
| Shape of coarse aggregate | NPD |  | Dangerous substances | NPD |
| Particle density (app,od,ssd) | 2.57,2.50,2.53 Mg/m3 (approx.) |  | Resistance to freezing & thawing | MS25 (coarse) XX (fine) |
| Water absorption | WA242 |  | Alkali-silica reactivity | Non-reactive |

The performance of the product identified above is in conformity with the set of declared performance/s. This declaration of performance is issued, in accordance with Regulation (EU) No 305/2011, under the sole responsibility of the manufacturer identified above.

Signed for and on behalf of the manufacturer by Clement Gavin	                                                                                                                                                                        At Kilmeague, Naas, Co. Kildare, Ireland

(Signature)

This DoP covers only the harmonised/mandated properties listed in Table ZA.1 of  I.S. EN 13139.                                                                               Information regarding other properties is available on request.